## Slide 1: METODE ROTIRAJUĆEG DISKA I ROTIRAJUĆEG PRSTEN-DISKA
Biljana Šljukić Paunković
Fakultet za fizičku hemiju
E-mail: biljka@ffh.bg.ac.rs
Notes: <number>

## Slide 2
<number>
Jednostavni elektrohemijski procesi - procesi u kojima se kao spori stupnjevi javljaju samo jednostepena izmena naelektrisanja i transport mase, zasebno ili istovremeno.
Složeni elektrohemijski procesi - spori stupanj predstavlja neki drugi tip procesa, npr. višeelektronska reakcija sa višestepenom izmenom elektrona, adsorpcija, hemijske reakcija, kristalizacija itd.
ELEKTROHEMIJSKI SISTEM I ELEKTROHEMIJSKA REAKCIJA
Notes: <number>

## Slide 3
<number>
Dva neizostavna stupnja elektrohemijske reakcije
Stupanj razmene elektrona i
Stupanj prenosa mase
Difuzija
Migracija
Konvekcija
ELEKTROHEMIJSKA REAKCIJA
Notes: Mass Transport
Transport of the reactants to the electrode and products from the electrode occurs by three different manners: diffusion, convection and migration.
Diffusion is the spontaneous movement of the solution under the influence of concentration gradient. Initially, before any potential is applied, the composition of the solution surrounding the electrode is homogeneous. When a potential is applied to the electrode so as to bring about electrolysis, a concentration gradient is set up and mass transport occurs from regions of high concentration to regions of lower concentrations, aimed to minimise concentration difference. Fick [9] proposed two experimentally based laws to predict the diffusion of a species. The diffusive flux, Jd, is related to the electrical current, I, by the expression:
(1.1)
where n is the number of electrons transferred, A is the electrode surface area and F is the Faraday constant. Fick’s first law defines the diffusive flux as:
(1.2)
where D is the diffusion coefficient and the concentration gradient. Fick’s second law expresses the variation of the concentration at a point as a function of time:
(1.3)
This indicates that the magnitude of the observed peak or limiting current is dependent upon the value of diffusion coefficient, which is a function of the solvent medium, the molecular weight of the electroactive species, the temperature, the electrolyte and the molecular dimensions.
Convection is flow of the solution to the electrode caused by mechanical forces. Natural convection is caused by differences in temperature or density of different regions of the solution. This type of solution flow is usually only found to be significant in experiments conducted over long time scales (> 10s) [10]. It can have an undesirable effect as its contribution to the current is unpredictable and irreproducible. This can be overcome either by conducting experiments on a relatively short timescale or by applying a method of forced convection. Mass transport by convection can also be introduce in the solution by stirring or flow of the solution and with rotation or vibration of the electrode, i.e. forced convection. To induce forced convection into electrochemical cell, rotating disc electrodes [11], channel [12] and high-speed flow [13] electrodes, and insonated electrodes [14] are commonly employed.
Migration is movement of charged species in the solution along an electrical potential gradient, . When a potential is applied to a cell then an electric field is developed at the electrode – solution interface resulting in a potential drop across the phase boundary. This will cause an electrostatic force on any ions or partially charged species in the solution, which in turn induces movement either to or from the electrode. The total migrative flux, Jm, is dependant on the concentrations of the ions, ci and their charges zi:
(1.4)
where R is the molar gas constant and T is the absolute temperature. Migration is usually undesirable in electrochemical experiments as varying the potential at the electrode alters the rate of migration making interpretation of voltammetric data difficult. Migration effects can be diminished by adding an excess of electrolytically inert ion known as supporting electrolyte, [15] normally in a concentration of ca. 100 times the concentration of species of interest (usually 0.1 M). This ensures that virtually the entire migrational contribution to the current comes from the supporting electrolyte rather than the electroactive species of interest. Furthermore the high concentration of the ionic electrolyte compresses the electrical double layer to very small values of only ca. 10 to 20 Å. The bulk solution is thus shielded from the charged surface of the electrode so that very little migration occurs within the bulk solution; consequently the full electrode potential is available to an electroactive species that has diffused to the surface of the electrode to drive electron transfer.
<number>

## Slide 4
<number>
Benjamin Levich
Broj publikacija sa metodom rotirajućeg diska po godini
Dr Benjamin Levich - pionir hidrodinamičke elektrohemije 1950tih.
„Fizičkohemijska hidrodinamika“
METOD ROTIRAJUĆEG DISKA
Notes: Veniamin Grigorievich (Benjamin) Levich was a leading scientist in electrochemical hydrodynamics, - invented and developed by him. The famous Levich equation describing a current at a rotating disk electrode is named after him.
<number>

## Slide 5: LINEARNA I CIKLICNA VOLTAMETRIJA
Promena potencijala sa vremenom u linearnoj voltametriji (A) sa tipičnim linearnim voltamogramom za n-elektronski redukcioni proces (B)
Promena potencijala sa vremenom u cikličnoj voltametriji (A) sa tipičnim cikličnim voltamogramom za n-elektronski redukcioni proces (B)

## Slide 6: METOD ROTIRAJUĆEG DISKA
<number>
http://compton.chem.ox.ac.uk/john/Thesis/1-figs/rde.gif
Au, staklasti ugljenik ili Pt
Teflon
Brzina rotacije!
Notes: RDE is constructed from a disk of electrode material (e.g. gold, glassy carbon or platinum) imbedded in a rod of insulating material (e.g. Teflon). The electrode is attached to a motor and rotated at a certain frequency. The movement of rotation leads to a very well defined solution flow pattern. The rotating device acts as a pump, pulling the solution upward and then throwing it outward.
It is important to note that the layer of solution immediately adjacent to the surface of the electrode behaves as if it were stuck to the electrode. While the bulk of the solution is being stirred vigorously by the rotating electrode, this thin layer of solution manages to cling to the surface of the electrode and appears (from the perspective of the rotating electrode) to be motionless. This layer is called the stagnant layer in order to distinguish it from the remaining bulk of the solution.
Hydrodynamic electrodes employ some form of forced convection to enhance mass transport of the reactants to the electrode. Therefore the rate of mass transport may be altered simply by adjusting the flow rate or electrode rotation rate. Also, steady state conditions are achieved rapidly, reducing problems with double layer charging currents.
<number>

## Slide 7
<number>
Transport mase ka elektrodi u slučaju rotirajućeg diska
jd,0 = 0.620 n F D2/3 ω1/2 v–1/6 C
n – broj razmenjenih elektrona
F – Faradejeva konstanta
D – koeficijent difuzije aktivne vrste
ω – ugaona brzina rotacije (rad/s)
v - kinematička viskoznost, tj. odnos viskoznosti rastvora i njegove gustine (cm2/s)
C – koncentracija aktivne vrste
x - rastojanje normalno na površinu elektrode
Levich-ova jednačina
+
Notes: vortex flow in the bulk solution continuously brings fresh analyte to the outer edge of the stagnant layer.
difuzija kroz difuzioni sloj do elektrode (tanji difuzioni sloj – aktivna vrsta brže prolazi kroz njega do elektrode)
The act of rotation drags material to the electrode surface where it can react. Providing the rotation speed is kept within the limits that laminar flow is maintained then the mass transport equation is given by
where the x dimension is the distance normal to the electrode surface. It is apparent that the mass transport equation is now dominated by both diffusion and convection and both these terms effect the concentration of reagent close to the electrode surface. Therefore to predict the current for this type of electrode we must solve this subject to the reactions occurring at the electrode.
Faster electrode rotation makes the stagnant layer thinner. faster rotation rates permit the analyte to diffuse to the electrode faster, resulting in a higher current being measured at the electrode.
Rotated disk voltammetry is similar to cyclic voltammetry in that the working electrode potential is (slowly) swept back and forth across the formal potential of analyte.
The Levich equation This equation takes into account both the rate of diffusion across the stagnant layer and the complex solution flow pattern. In particular, the Levich equation gives the height of the sigmoidal wave observed in rotated disk voltammetry. The sigmoid wave height is often called the Levich current, iL, and it is directly proportional to the analyte concentration, C. The Levich equation is written as:
iL = (0.620) n F A D2/3 w1/2 v–1/6 C
where w is the angular rotation rate of the electrode (radians/sec) and v is the kinematic viscosity of the solution (cm2/sec). The kinematic viscosity is the ratio of the solution's viscosity to its density.
The rotating disk electrode (RDE) is one example of a hydrodynamic electrode. The actual electrode itself, comprised of a disk electrode surrounded by an insulating sheath, imposes the motion as the name implies; the disk is rotated around the axis perpendicular to its plane with an angular velocity, . A laminar flow is established as the rotation forces solution out from the outer sheath in a radial direction, pulling fresh material towards the working surface. The rotation rate influences the rate of mass transfer and consequently it influences the thickness of the diffusion layer :
(1.18)
where is the kinematic viscosity in m2s-1. When the equation (1.18) is substituted in the equation for the diffusion limited current in case of a stationary electrode, it gives Levich equation [28, 29] that describes diffusion limited current in case of rotating disc electrode:
(1.19)
The equation (1.19) shows that diffusion limited current can be influenced not only by concentration of the reactant as in case of stationary diffusion, but also rotation rate, reducing the diffusion layer thickness. The thickness of the diffusion layer at the rotating disc electrode is two to three orders of magnitude smaller than in case of a stationary electrode [30].
<number>

## Slide 8
<number>
Levich plot
A = 0.1963 cm2
C = 2.55x10–6 mol/cm3
v = 0.00916 cm2/s
D = 4.75x10–6 cm2/s
Notes: results for a series of rotated disk voltammograms taken at different scan rates.
a Levich study. The limiting current (or Levich current) is measured and plotted against the square root of the rotation rate, producing a Levich plot. Note that the experimental rotation rate, f , is measured in RPM and must be converted to the angular rotation rate, w, so that it has units of radians per second
in experiment shown the electrode area, A, was 0.1963 cm2, the analyte concentration, C, was 2.55x10–6 mol/cm3, and the solution had a kinematic viscosity, v, equal to 0.00916 cm2/sec. After careful substitution and unit analysis, you can solve for the diffusion coefficient, D, and obtain a value equal to 4.75x10–6 cm2/s.
<number>

## Slide 9
<number>
za ω u rpm
ik,0 – kinetička gustina struje (mA cm-2)
i0 – gustina struje izmene (mA cm-2)
α – koeficijent prenosa naelektrisanja u odlučujućem stupnju
Eeq – ravnotežni elektrodni potencijal
R – univerzalna gasna konstanta
T – temperatura (K)
Koutecky – Levich jednačina
U slučaju neograničene difuzije
Notes: <number>

## Slide 10
<number>
E = f (ln(ik,0))
n - broj razmenjenih elektrona
α – koeficijent prenosa naelektrisanja
i0 – gustina struje izmene
***********************
D - koeficijent difuzije
v – kinematička viskoznost
1/id,0 = f(ω-1/2)
ik,0 – kinetička gustina struje
I0 – gustina struje izmene

## Slide 11
<number>

## Slide 12
<number>
U slučaju film elektrode:

## Slide 13: Granice RDE metode
<number>
Za v = 0.01 cm2 s-1 i r = 0.25 cm, w > 1.6 s-1 ili w>9.7 rpm
Za v = 0.01 cm2 s-1 i r = 0.25 cm, w <3.2 x 104 s-1 ili w <3.06 x 105 rpm
Granice u praksi: 100 rpm < w < 10 000 (4 000) rpm

## Slide 14: METOD ROTIRAJUĆEG PRSTEN-DISKA
<number>
(P) Prsten
(D) Disk
dP
dD
dP = dD
r1 – radijus diska
r2 – unutrašnji radijus prstena
r3 – spoljašnji radijus prstena
Notes: Rotating-ring-disk electrode: A variant of the rotating-disk electrode which includes a second electrode - a concentric ring electrode - that is placed outside the disk and used to analyze the species generated on the disk. The ring is electrically insulated from the disk so that their potentials can be controlled independently. Abbreviated as RRDE
convenient way to measure post-electron transfer reactions of products
relationship between disk current and ring current depends on rate of movement of product from the disk
only a fraction of disc products will reach ring
each ring-disk electrode must be calibrated with a well-behaved reversible couple to determine the collection efficiency (N)
N= iR / iD
couples used - ferri/ferocynadide, quinone/hydroquinone
efficiency depends on electrode geometry (radii of disk and ring)
<number>

## Slide 15
<number>
KOLEKCIONI EKSPERIMENTI
Vrste nastale na disk elektrodi za vreme nekog od redoks procesa se detektuju (kolektuju) u uslovima potpune konvektivno-difuzione kontrole na nezavisno potenciostatski kontrolisanoj prstenastoj elektrodi.
EPrsten na potencijalu koji ima dovoljno pozitivnu vrednost da će se oksidovati R.
iD,c O + ne R
ERing
iD,lim
+ - EDisk vs. Ref
iR,lim
R O + ne
iR,a
Notes: KOLEKCIONI EKSPERIMENTI. U ovom tipu eksperimenata, vrste nastale na disk elektrodi za vreme nekog od redoks procesa se detektuju (kolektuju) u uslovima potpune konvektivno-difuzione kontrole na nezavisno potenciostatski kontrolisanoj prstenastoj elektrodi. Zavisno od veličina r1, r2 i r3, na prstenastoj elektrodi se detektuje samo deo ukupne količine vrsta nastalih na disk elektrodi. Odnos struja prstenaste elektrode u odnosu na struju disk elektrode naziva se kolekciona efikasnost:
(5)
Uobičajeni način eksperimentalnog odredjivanja veličine N je oksidacija heksacijanoferata(II) (sa Fe2+ kao centralnim jonom) na prstenastoj elektrodi, na potencijalu koji odgovara difuzionoj kinetici, (na pr. +0.4 V prema slici 2), koji se formira na disk elektrodi reakcijom redukcije heksacijanoferata(III) (Fe3+), pri čemu potencijal diska odgovara difuziono kontrolisanoj redukciji (na pr. -0.1 V prema slici 2). Koleksiona efikasnost je tada prosto odnos jačine struje prstena i struje diska. Kolekciona efikasnost se takođe može i terijski izračunati, korišćenjem relativno komplikovanog izraza, koji zavisi samo od radijusa disk i prstenaste elektrode.
<number>

## Slide 16
<number>
KOLEKCIONI EKSPERIMENTI
Kolekciona efikasnost N - odnos struja prstenaste elektrode u odnosu na struju disk elektrode.
I = 20 – 40%
I-E krive kvazireverzibilnog redoks sistema Fe(CN)63-/Fe(CN)64- iste koncentracije 10-2 M, u osnovnom rastvoru 0,5 M KCl, na rotirajućem Pt disku za različite frekvencije obrtanja.
Određivanje kolekcione efikasnosti
Notes: KOLEKCIONI EKSPERIMENTI. U ovom tipu eksperimenata, vrste nastale na disk elektrodi za vreme nekog od redoks procesa se detektuju (kolektuju) u uslovima potpune konvektivno-difuzione kontrole na nezavisno potenciostatski kontrolisanoj prstenastoj elektrodi. Zavisno od veličina r1, r2 i r3, na prstenastoj elektrodi se detektuje samo deo ukupne količine vrsta nastalih na disk elektrodi. Odnos struja prstenaste elektrode u odnosu na struju disk elektrode naziva se kolekciona efikasnost:
(5)
Uobičajeni način eksperimentalnog odredjivanja veličine N je oksidacija heksacijanoferata(II) (sa Fe2+ kao centralnim jonom) na prstenastoj elektrodi, na potencijalu koji odgovara difuzionoj kinetici, (na pr. +0.4 V prema slici 2), koji se formira na disk elektrodi reakcijom redukcije heksacijanoferata(III) (Fe3+), pri čemu potencijal diska odgovara difuziono kontrolisanoj redukciji (na pr. -0.1 V prema slici 2). Koleksiona efikasnost je tada prosto odnos jačine struje prstena i struje diska. Kolekciona efikasnost se takođe može i terijski izračunati, korišćenjem relativno komplikovanog izraza, koji zavisi samo od radijusa disk i prstenaste elektrode.
<number>

## Slide 17
<number>
KOLEKCIONI EKSPERIMENTI
Zavisi od geometrije elektrode
Ne zavisi od w, C, D, etc. ako je R konstantan
Ako R → Z, onda je Nexp < Ntheor i N = F(w).
Određivanje kolekcione efikasnosti
Notes: Uobičajeni način eksperimentalnog odredjivanja veličine N je oksidacija heksacijanoferata(II) (sa Fe2+ kao centralnim jonom) na prstenastoj elektrodi, na potencijalu koji odgovara difuzionoj kinetici, (na pr. +0.4 V prema slici 2), koji se formira na disk elektrodi reakcijom redukcije heksacijanoferata(III) (Fe3+), pri čemu potencijal diska odgovara difuziono kontrolisanoj redukciji (na pr. -0.1 V prema slici 2). Koleksiona efikasnost je tada prosto odnos jačine struje prstena i struje diska. Kolekciona efikasnost se takođe može i terijski izračunati, korišćenjem relativno komplikovanog izraza, koji zavisi samo od radijusa disk i prstenaste elektrode.
<number>

## Slide 18
<number>
EKSPERIMENT ZAKLANJANJA
Faktor zaklanjanja
Praćenje iste reakcije na prstenastoj i na disk elektrodi
EPrsten na vrednosti koja odgovara graničnoj konvektivno-difuzionoj struji redoks procesa.
Struja na prstenastoj elektrodi u uslovima kada je struja diska Idisk = 0, tzv. nezaklonjena (unshielded) struja prstena:
Granična struja prstenaste elektrode u uslovima IDisk ≠ 0
Struja prstenaste elektrode u uslovima kada Idisk odgovara graničnoj konvektivno-difuzionoj struji
Razdvajanje ukupne struje disk elektrode na komponente koje odgovaraju pojedinačnim procesima!
β = r33/r13-r23/r13
Notes: EKSPERIMENT ZAKLANJANJA. Kod ovog tipa eksperimenata na prstenastoj i disk elektrodi prati se odigravanje iste redoks reakcije. Potencijal prstenaste elektrode nalazi se na vrednosti koja odgovara graničnoj konvektivno-difuzionoj struji redoks procesa. Kada se potencijal disk elektrode nalazi na vrednosti na kojoj se dati proces ne odigrava, tj na vrednosti na kojoj je IDisk=0, struja koja se detektuje na prstenastoj elektrodi se naziva nezaklonjena (unshielded) struja prstena, koja je u vezi sa graničnom strujom diska, Id,Disk, ukoliko bi se na njoj odigravala reakcija, preko jednačine:
(6)
Ukoliko se, sada, disk elektroda nađe na potencijalu na kome IDisk≠0 fluks elektroaktivne vrste koji dolazi do prstenaste elektrode biće umanjen kao posledica njenog trošenja u redoks procesu na disk elektrodi. Veličina ovog smanjenja biće jednaka fluksu proizvoda reakcije na disku u uslovima kolecionih RDEP eksperimenata, tj –NIDisk. Zbog toga se za graničnu struju prstenaste elektrode u uslovima kada IDisk nije jednaka nuli dobija:
(7)
U specijalnom slučaju kada struja diska odgovara graničnoj konvektivno-difuzionoj struji, za struju prstena se dobija da je jednaka:
(8)
Faktor Nβ-2/3 u zagradi predhodnog izraza, zove se FAKTOR ZAKLANJANJA, dok N ima uobičajeno značenje kolekcione efikasnosti. Eksperimenti zaklanjanja omogućuju, dakle, razdvajanje ukupne struje disk elektrode na komponente koje odgovaraju pojedinačnim procesima.
β konstanta bazirana na radijusima disk elektrode i prstena (β=r33/r13-r23/r13)
<number>

## Slide 19
<number>
http://electrochem.cwru.edu/ed/encycl/fig/c01/c01-f05b.jpg
Katalizatori za gorivne ćelije
http://gladiator.ncsa.uiuc.edu/Images/nuggets/1a.jpg

## Slide 20: GORIVNE ĆELIJE
<number>
Notes: Gorivne ćelije su elektrokemijski uređaji za neposrednu pretvorbu kemijske energije vodika i kisika u istosmjernu električnu energiju, a kao dodatni proizvod nastaje voda. Gorivne ćelije se kao i baterije sastoje od anode, katode i elektrolita, samo što za razliku od baterija ne čuvaju kemijsku energiju, nego kemijsku energiju goriva pretvaraju u električnu energiju. Stoga, gorivnim ćelijama nije potrebno punjenje kako bi mogle proizvoditi električnu energiju, već je proizvode sve dok je prisutno gorivo i kisik. Kao gorivo se najčešće koristi vodik zbog visoke reaktivnosti, što smanjuje potrebu skupog katalizatora. Instalirana snaga elektrana s gorivnim ćelijama koje proizvode električnu i toplinsku energiju ovise o njihovoj izvedbi, a mogu imati raspon snage čak od 1 kW do 10 MW. Popularizacija korištenja vodika kao "goriva budućnosti" potiče automobilske tvrtke da sve više razvijaju motore na hibridni pogon.
<number>

## Slide 21
<number>
RRDE: Ugljenični disk, platinski prsten
Disk elektroda se pokriva filmom koji sadrži nanočestice platine ili nekog drugog ispitivanog elektrokatalizatora
Velika brzina rotacije povlači rastvoren O2 ka elektrodi
http://gladiator.ncsa.uiuc.edu/Images/nuggets/1a.jpg
Tok rastvorenog
O2 ka elektrodi

## Slide 22
<number>
Direktna ili četvoro-elektronska redukcija kiseonika:
U alkalnim rastvorima:
O2 + 2H2O + 4e- = 4OH- ; E0 = + 0,401 V
U kiselim rastvorima:
O2 + 4H+ + 4e- = 2H2O; E0 = + 1.229 V
Dvo-elektronska redukcija kiseonika ili peroksidni put:
U alkalnim rastvorima:
O2 + H2O + 2e- = HO2- + OH- E0 = -0.065 V
što je praćeno bilo daljom redukcijom:
HO2- + H2O + 2e- = 3OH-- E0 =+ 0.867 V
ili razlaganjem prema reakciji:
2HO2- = 2OH- + O2
U kiselim rastvorima:
O2 + 2H+ + 2e- = H2O2- E0 = + 0.67 V
nakon čega sledi:
H2O2 + 2H+ + 2e- = 2H2O - E0 = + 1.77 V
ili:
2H2O2 = 2H2O + O2
Notes: Reakcija redukcije kiseonika je istraživana na različitim površinama, kao što su elektroda od platine, žive, srebra, zlata i elektrode na bazi ugljeničnih materijala. Nađeno je da na elektrohemijsku redukciju kiseonika utiču kako materijal elektrode tako i elektrolitički rastvor. Uticaj elektrodnih materijala i različitih rastvarača na elektrohemijsku redukciju kiseonika kroz njihov uticaj na potencijal i struju redukcionog pika je detaljno proučavan. Medjutim, detaljan mehanizam reakcije redukcija kiseonika je još uvek nejasan. Generalno se veruje da se redukcija kiseonika odvija ili kao četvoro
Ugljenične elektrode su od velikog interesa za redukciju kiseonika jer su korišćene kao nosači za platinske katalizatore u gorivim ćelijama. Međutim, redukcija kiseonika na ugljenčnim elektrodama se prevashodno odvija kao dvo-elektronski poces dajući vodonik-peroksid, koji je neželjen proizvod u gorivnim ćelijama jer smanjuje energetsku efikasnost ćelija.(26,27) Stoga su ugljenične elektrode pogodne za elektrohemijsku sintezu vodonik peroksida. – elektronski proces dajući vodu kao krajni proizvod ili kao dvo-elektronski proces sa vodonik–peroksidom kao krajnjim produktom
U cilju analize uticaja prirode metala i pH vrednosti na RRK često se koristi pojednostavljena shema na slici 3, predložena od strane Vroblove (Wroblova) i saradnika, primenljiva kako u kiselim tako i u alkalnim rastvorima
Na osnovu ove reakcione sheme, O2 koji de adsorbuje na površini platinske elektrode može se elektrohemijski redukovati ili direktno do vode, sa konstantom brzine k1, uz utrošak 4 elektrona po molekuli O2, bez formiranja H2O2 kao intermedijera (to je tzv. ‘’direktna’’ 4e- redukcija) ili do adsorbovanog peroksida, H2O2,ad, uz utrošak 2 elektrona, sa konstantom brzine k2 (‘’serijska’’ 2e- redukcija), uz dalju redukciju apsorbovanog peroksida do vode, uz utrošak još dva elektrona sa konstantom brzine k3 (‘’serijski’’ 4e- reakcioni put). Adsorbovani peroksid se može osim redukcije još i katalitički (hemijski) razložiti na površini elektrode, konstantom brzine k4, ili desorbovati sa elektrode u rastvor elektrolita ( konstanta brzine k5). Direktna 4e- redukcija zaheva disocijaciju molekularnog kiseonika pre transfera prvog elektrona. S obzirom na veliku energiju disocijacije O2, ovaj tip reakcionog puta favorizovan je na metalima kod kojih je energija inerakcije M-O veoma jaka, ne manja od 250 kJ/mol. Međutim, metali sa veoma jakom vezom M-O imaju slabu aktivnost za reakciju redukcije kiseonika, zbog toga što se reakcija prekida formiranjem površinskog OHad., tj reakcija postaje ograničena sporošću desorpcije kiseoničnih vrsta sa površine. Energetski povoljniji reakcioni put je superokso/perokso put, sa transferom prvog elektrona na molekul kiseonika. Energija disocijacije O2,ad- i/ili O2,ad2- je mnogo niža od energije disocijacije molekularnog kiseonika (za odprilike 100 kJ/mol), što rezultuje u relativno brzoj kinetici redukcije kiseonika bez zahteva za jaku M-O vezu. Peroksidni intermedijer, adsorbovan na površini, može ili ne mora biti dalje redukovan do vode, zavisno od relativnog odnosa brzina stupnjeva k4 i k5. Iako postoje brojna pitanja vezana za interpretaciju ovog reakcionog puta, veći broj studija ukazuju na serijski reakcioni put, preko formiranja peroksidnog, H2O2,ad, intermedijera kao operativnog puta reakcije redukcije kiseonika na čistim metalima platine, zlata, bakra i njihovih legura. Ovo se može smatrati specijalnim slučajem generalno predloženog mehanizma kod koga je k1 praktično jednaka nuli, tj do raskidanja O-O veze ne dolazi pre formiranja peroksidne vrste. U svakom slučaju, čini se da je kinetički odlučujući stupanj transfer prvog elektrona na O2 i formiranje superokso radikal anjona, O2,ad-:
(9)
Ovde je pretpostavljeno da je elektron transfer proces koji se odigrava u unurašnjoj sferi, tj do transfera elektrona dolazi sa metala na adsorbovanu vrstu na elektrodi. Zbog toga je ukupna aktivaciona energija procesa umanjena za energiju adsorpcije reakcionog intermedijera.
<number>

## Slide 23
<number>
James P. Collman, Richard A. Decréau, Chem. Commun., 2008, 5065
tok rastvorenogO2
Notes: Metoda diska i prstena je pogodna za ispitivanje mehanizma redukcije kiseonika. Naime vodonik peroksid je vrsta koja se može detektovati elektrohemijski pošto se može oksidovati do vode u difuziono kontrolisanom procesu. Ako se potencijal diska podesi na vrednost koja odgovara redukciji kiseonika, a potencijal prstena na vrednost koja odgovara oksidaciji vodonik peroksida difuzionom kinetikom, može se pratiti da li i u kojoj meri redukcija kiseonika teče do vode, a u kojoj samo do vodonik peroksida. Naime ako se redukcija kiseonika odigrava 4e- putem, dakle do vode, na prstenu se neće detektovati nikakva struja. Medjutim ako deo vodonik peroksida uspe da se desorbuje pre redukcije (k5 veća od 0), on će dolaziti do prstena i oksidovati se pa će struja prstena biće veća od nule. Poznavajući kolekcionu efikasnost može se iz odnosa struja prstena i diska tačno odrediti koja frakcija redukcije kiseonika teče 4e- a koja 2e- putem
<number>

## Slide 24
<number>
flow of dissolved
O2
Struje diska (ID) i struje prstena (IR) za redukciju kiseonika RRK na Pt(100) Pt(110) i Pt(111) u kiselim i alkalnoj sredini. [C.A. Lucas, N.M. Markovic, Encyclopedia of Electrochemistry, Vol.2, sect. 4.1.2.1.2., Wiley-VCH, 2004]
Notes: . Radi ilustracije slika 5 prikazuje ispitivanje redukcije kiseonika u rastvorima 0.05 M H2SO4, 0.1M HClO4 i 0.1 M KOH zasićenim kiseonikom, na monokristalnim površinama platine različitih Milerovih indeksa. Pošto je struja prstena jednaka nuli na svim potencijalima većim od 0.4 V u odnosu na vodoničnu referentnu elektrodu, to znači da na tim potencijalima redukcija teče 4e- putem. Na potencijalima manjim od 0.4 V pojavljuje se struja prstena, što znači da se smanjuje udeo 4e- a pojavljuje udeo 2e- puta. To je izrazito za neke ravni, na primer za Pt(111) u H2SO4 ili Pt(110) u HClO4, i ravni Pt (110) i (100) u alkalnoj sredini. Pojava gubitaka reakcionog intermedijera , odnosno nepotpuna redukcija do vode, znači i manji utrošak elektrona po molekuli redukovanog kiseonika što se očituje kao smanjenje struje diska (sl. 5)
<number>

## Slide 25: DIREKTNE BORHIDRIDNE GORIVNE ĆELIJE
<number>
Ukupna reakcija:
BH4- + OH- → BO2- + 2H2O (E0 = 1.64 V)
Reakcija na katodi
reakcija redukcije kiseonika:
O2 + 2H2O + 8e- → 8OH- (E0 = 0.41 V)
ili redukcije vodonik peroksida (H2O2):
4H2O2 + 8H+ + 8e- → 8H2O

## Slide 26
U DBFC dolazi do oksidacije BH4- u metaboratni jon, BO2-, na anodi čime se oslobodi najviše 8e-.
BH4- + 8OH- → BO2- + 6H2O + 8e- (E0 = - 1.24 V)
nedostatak ovog anodnog procesa jeste izdvajanje vodonika (H2) i hidroksiborata (BH3(OH)-), tj. hidroliza NaBH4:
BH4− + H2O → BH3OH− + H2

## Slide 27
<number>
Notes: <number>